M. Tassawur Hassnain

001335-005 BTTM (H)

Dyeing Polyester 
with PROsperse Disperse Dye
Please read directions carefully before starting
· Wear rubber gloves, apron or old clothes.
· Utensils used for dyeing should never be used for food preparation.
SUPPLIES
PROsperse Disperse Dye PRO Dye Carrier ADP
Metaphos Acetic Acid 56% OR Citric Acid Crystals
Synthrapol
Procedure:
1. Machine wash fabric on HOT cycle, minimum temperature of 140*F (60*C), or by hand in a pot on the stove, with 1/2 tsp. (2 gm) PRO Dye Activator and 1/2 tsp (2.5 ml) Synthrapol per pound of fabric (454 gm, or 3 to 4 yards muslin weight fabric)
Removing Permanent Press finish: If your fabric has a permanent press finish on it, you will need to remove it prior to dyeing, otherwise continue with step #6. WARNING: Use rubber gloves and protective eye ware when handling acid. Use extra caution!!!
2. Treat 1 pound (454 gm) of fabric in a solution of hydrochloric (muriatic) acid that is 30% to 35% strength, prepared by CAREFULLY adding 1 tablespoon (15 ml) of the acid to 2 gallons (8 liters) of cool water. Use a stainless steel or enamel pot.
3. Add the washed fabric and heat to 185*F (85*C) with intermittent stirring for twenty minutes.
4. Rinse thoroughly in warm water.
5. Extract water and add fabric to dyebath.
Solid Shade Immersion Dyeing for 1 pound (454 gm) 100% Polyester:
PROsperse dye: 1/2 tsp to 6 tsp (1.25 gm to 15 gm), depending on desired shade
1/2 tsp (2.5 ml ) Synthrapol 
1 tsp (5 ml) Acetic Acid 56% OR 1 tsp (5.8 gm) Citric Acid Crystals
2 Tbl (30 ml) PROdye Carrier ADP
1/2 tsp (3.5 gm) Metaphos 
2 1/2 gallons (10 liters) water
6. Dissolve the dye in 1 cup (250 ml) hot 140*F (60*C) but NOT boiling water before adding to dye bath. Strain through two layers of old nylon stockings. Let stand while preparing the rest of the dyebath.
7. Heat your dye bath with warm 120*F (49*C) water. Dissolve the PROdye Carrier ADP in 1 cup (250 ml) boiling water. Add Synthrapol SP, Acetic Acid 56% and Metaphos. STIR WELL!
8. While stirring constantly, bring dye bath rapidly to a boil. Simmer 30 to 45 minutes. Stir intermittently.
9. Remove from heat and immediately rinse the fabric in a pan of very HOT 160*F (71*C) water. 
10. Then wash with 1/2 tsp (2.5 ml)Synthrapol SP in very HOT 160*F (71*C) water
11. Rinse and dry fabric..
All Dyeing should be carried out in a stainless steel or enamelware container only. Never use aluminum pots. Use Pyrex or stainless steel measuring utensils and a large wooden dowel for stirring in the boiling dye bath. Provide for good VENTILATION DURING THE ENTIRE DYEING CYCLE!
