Simple Cubic Lattice

Crystalline solids are those solids, unlike amorphous solids, that have a regular and repeating arrangement of atoms.  Each of these crystalline solids consists of a unit cell which is a small group of atoms that contain unique features.  When a large number of these unit cells are stacked together, they form a macroscopic crystal.  The three cubic crystal types are the simple cubic lattice (primitive cubic), body-centered cubic, and the face-centered cubic.  The simple cubic unit cell is shown below.

The length of a side of the unit cell, a, is called the lattice constant.  An important feature of a crystal structure is the nearest distance between atomic centers

(nearest-neighbor distance) and for the primitive cubic this distance is a.

A simple cubic lattice has eight lattice points where a lattice point is defined as a point of intersection of two or more grid lines.  Each lattice point, eight in the diagram above, is a “site” for an atom to reside.  However, the unit cell above does not contain 8 atoms but only 1.  When considering cubic lattices, one must always think in terms of 3-D.  Atoms at the corners of any cube are shared by 8 contiguous units cells, so only 1/8 of an atom is attributed to a single lattice point.  Therefore,

1/8 atom/lattice point × 8 lattice points = 1 atom

An interesting property of primitive cubic cells is that of packing efficiency where

PE = Va/Vuc × 100%

and Va is the volume of the atoms occupying the interior of the cell and Vuc 	is the volume of the unit cell.

Va = 4/3•π•r3•Z where r is the atomic radius and Z the number of atoms 	contained within the unit cell.

Vr = l•w•h = w•w•w = (2r)3 = 8r3

PE = 4/3•π•r3•Z/8r3 × 100% = 52% which applies to all primitive cubic cells.

The graphic used in this tutorial was taken from the Crystal Lattice Structures Web page, http://cst-www.nrl.navy.mil/lattice/ provided by the Center for Computational Materials Science of the United States Naval Research Laboratory.

# Text boxes

a

The length of each side is a (2r) where r is the radius of the atom at the

lattice point.

lattice point

a